# Appendix D

Material Properties

_____________________________________________________________________________________________________

Conductivity

The conductivity for a variety of common conductive materials are given in Table D.1.  These values are typical at room temperatures and for low frequencies.  More detailed specifications can be found in a variety of handbooks.

| MATERIAL (Metals) |  - (m)-1 |
| --- | --- |
| Silver | 6.17x107 |
| Copper | 5.80x107 |
| Gold | 4.10x107 |
| Aluminum | 3.82x107 |
| Tungsten | 1.82x107 |
| Zinc | 1.67x107 |
| Brass | 1.50x107 |
| Nickel | 1.45x107 |
| Iron | 1.03x107 |
| Phosphor Bronze | 1x107 |
| Solder | 0.7x107 |
| Carbon Steel | 0.6x107 |
| German Silver | 0.3x107 |
| Manganin | 0.227x107 |
| Constantan | 0.226x107 |
| Germanium | 0.22x107 |
| Stainless Steel | 0.11x107 |
| Nichrome | 0.1x107 |

| MATERIAL (Non-metals) |  - (m)-1 |
| --- | --- |
| Graphite | 7x104 |
| Silicon | 1200 |
| Ferrite (typical) | 100 |
| Water (sea) | 5 |
| Limestone | 10-2 |
| Clay | 5x10-3 |
| Water (fresh) | 10-3 |
| Water (distilled) | 10-4 |
| Soil (sandy) | 10-5 |
| Granite | 10-6 |
| Marble | 10-8 |
| Bakelite | 10-9 |
| Porcelain (dry process) | 10-10 |
| Diamond | 2x10-13 |
| Polystyrene | 10-16 |
| Quartz | 10-17 |

Permittivity

The relative permittivity for a variety of common dielectric materials are given in Table D.2.  These values are typical at room temperatures and for low frequencies.  More detailed specifications can be found in a variety of handbooks.

| MATERIAL | Relative Permittivity - R |
| --- | --- |
| Air | 1.0005 |
| Alcohol, ethyl | 25 |
| Aluminum oxide | 8.8 |
| Amber | 2.7 |
| Bakelite | 4.74 |
| Barium titanate | 1200 |
| Carbon dioxide | 1.001 |
| Ferrite (NiZn) | 12.4 |
| Germanium | 16 |
| Glass | 4-7 |
| Ice | 4.2 |
| Mica | 5.4 |
| Neoprene | 6.6 |
| Nylon | 3.5 |
| Paper | 3 |
| Plexiglas | 3.45 |
| Polyetheylene | 2.26 |
| Polystyrene | 2.56 |
| Porcelain (dry process) | 6 |
| Pyranol | 4.4 |
| Pyrex glass | 4 |
| Quartz (fused) | 3.8 |
| Rubber | 2.5-3 |
| Silica or SiO2 (fused) | 3.8 |
| Silicon | 11.8 |
| Snow | 3.3 |
| Sodium chloride | 5.9 |
| Soil (dry) | 2.8 |
| Steatite | 5.8 |
| Styrofoam | 1.03 |
| Teflon | 2.1 |
| Titanium Dioxide | 100 |
| Water (distilled) | 80 |
| Wood (dry) | 1.5-4 |

Permeability

The relative permeability for a variety of common magnetic materials are given in Table D.3.  These values are typical at room temperatures and for low frequencies.  More detailed specifications can be found in a variety of handbooks.

| MATERIAL | Relative Permeability - R |
| --- | --- |
| Bismuth | .9999986 |
| Paraffin | .99999942 |
| Wood | .9999995 |
| Silver | .99999981 |
| Aluminum | 1.00000065 |
| Beryllium | 1.00000079 |
| Nickel chloride | 1.00004 |
| Manganese sulfate | 1.0001 |
| Nickel | 50 |
| Cast iron | 60 |
| Cobalt | 60 |
| Powdered iron | 100 |
| Machine steel | 300 |
| Ferrite (typical) | 1000 |
| Permalloy 45 | 2500 |
| Transformer iron | 3000 |
| Silicon iron | 3500 |
| Iron (pure) | 4000 |
| Mumetal | 20000 |
| Sendust | 30000 |
| Supermalloy | 100000 |